## Slide 1: Choosing cowinding
For 14T magnet

## Slide 2
Fieldstrength: 14.1T
Wire: 485.6km
Hom. 1.77ppm
Magnet Design: (genetic+spline from scratch)

## Slide 3
Hoopstress evalution (14T Setup, ~Lis design):

## Slide 4
Options for Co-Winding Material |  | 
 | E-Modul in Gpa bei 20°C | E-Modul in Gpa bei 8 Kelvin
Molybdän (Mo) = Mo-Band | 329 | 361.9
MoH4-Band |  | 
MY-Band |  | 
MY-ESS-Band |  | 
HASTELLOY® C-276 alloy l NiMo16Cr15W l 2.4819 | 205-215 | 231
Durnomag = 1.4369 = X11CrNiMnN19-8-6 | 200 | 240
Edelstahl z.B. (X5CrNi18-10) - ca. 200-220 GPa | 200-220 | 231
Kupferlegierung hochfest CuMn20Ni20 | 160 - 180 | 187
CuNi C71500 | 150 | 160 bei 4 K
reines Kupfer = 2.0060 = Cu-ETP | 110 - 130 | ~130
Wolfram | 405 | 445.5

## Slide 5
Fresh result: Hoopstress simulation for our 14T settings:

## Slide 6: Path to final magnet design:
14T Magnet Design
Optim. Homogeneity and Wire consumption
Estimate Stresses
For Axial and Hoopstresses
Acoount for stresses
Incorporate cowinding (radial distriubution and material type)
Incorporate pressure disk distribution along z axis
Second optimization
Regain 14.1T & 1ppm homogeneity

## Slide 7
Magnet Design: (linear solver, global solution)
*2
*2
*2